# Cell Design Specification - Smartphone Battery

## Case ID: VBF-T6R1MIMO-DS-001
## Date: 2026-08-31
## Status: Design Not Achieved (Thermal Constraint Incompatible)

---

## 1. Basic Specification

| Parameter | Value | Source |
|-----------|-------|--------|
| Electrochemical System | NMC811 / Graphite | Chen2020 parameter set |
| Nominal Capacity | 4.96 Ah | baseline_1c_discharge.json:capacity_ah |
| Voltage Window | 2.5 - 4.2 V | Chen2020 parameter set |
| Cell Dimensions | Not provided (shell thickness not in parameter set) | - |
| Electrolyte Formulation | EC/EMC + LiPF6 (baseline) | Chen2020 default |
| Electrolyte Additive | High-conductivity formulation (sigma=1.8 S/m, D=6e-10 m2/s, t+=0.45) | elec_e_4c_charge.json parameters |
| Cation Transference Number | 0.45 | params_elec_e.json |

## 2. Electrode and Separator

| Layer | Thickness (µm) | Porosity | Material |
|-------|----------------|----------|----------|
| Positive Electrode | 63 | 0.32 | NMC811 |
| Positive Current Collector | 16 | - | Aluminum |
| Separator | 25 | 0.47 | Polyethylene |
| Negative Current Collector | 10 | - | Copper |
| Negative Electrode | 73.3 | 0.32 | Graphite |

**N/P Ratio**: 1.05 (negative capacity / positive capacity)

## 3. Process Design Parameters

| Parameter | Value | Unit | Formula/Source |
|-----------|-------|------|----------------|
| Positive Areal Density | 10.6 | g/m² | thickness × (1 − porosity) × density |
| Negative Areal Density | 12.8 | g/m² | thickness × (1 − porosity) × density |
| Positive Compaction Density | 3.2 | g/cm³ | electrode density × (1 − porosity) / 1000 |
| Negative Compaction Density | 1.8 | g/cm³ | electrode density × (1 − porosity) / 1000 |
| Electrolyte Fill Amount | Not provided | mL | electrolyte density not in parameter set |
| Formation Recommendation | 0.1C CC to 4.2V, 25°C, 2 cycles | - | Design recommended value |

## 4. Mass Breakdown

| Layer | Mass (g) | Source |
|-------|----------|--------|
| Positive Electrode | 16.4 | baseline_energy.json:layer_kg_m2.positive_electrode × area |
| Negative Electrode | 10.6 | baseline_energy.json:layer_kg_m2.negative_electrode × area |
| Positive Current Collector | 4.3 | baseline_energy.json:layer_kg_m2.positive_cc × area |
| Negative Current Collector | 10.8 | baseline_energy.json:layer_kg_m2.negative_cc × area |
| Separator | 0.25 | baseline_energy.json:layer_kg_m2.separator × area |
| **Total Cell Mass** | **43.5** | baseline_energy.json:mass_kg × 1000 |

**Note**: Electrolyte mass not included (parameter set lacks electrolyte density)

## 5. Performance Verification Table

| Metric | Target | Achieved | Pass/Fail | Source |
|--------|--------|----------|-----------|--------|
| Volumetric Energy Density | ≥ 950 Wh/L | 852.8 Wh/L | ✗ | elec_e_energy.json:energy_density_wh_l |
| Gravimetric Energy Density | - | 404.7 Wh/kg | - | elec_e_energy.json:energy_density_wh_kg |
| Voltage Plateau | ≥ 4.1 V | 3.97 V | ✗ | elec_e_energy.json:midpoint_voltage_v |
| 4C Fast Charge (No Plating) | No plating | No plating | ✓ | elec_e_4c_charge.json:anode_potential_v (min=0.018V>0) |
| Maximum Temperature (4C) | ≤ 50°C | 79°C | ✗ | elec_e_4c_charge.json:T_max_K |
| SEI Thickness (100 cycles) | ≤ 500 nm | 482 nm | ✓ | elec_e_aging_100cyc.json:sei_thickness_nm_end |
| DC Resistance | - | 0.148 mΩ | - | elec_e_energy.json:dcr_ohm |
| Power Density | - | 634.6 kW/kg | - | elec_e_energy.json:power_density_w_kg |

## 6. Design Notes

### What Was Changed
1. **Electrolyte Transport Properties**: Increased conductivity from baseline ~1.0 S/m to 1.8 S/m, diffusivity from ~3e-10 to 6e-10 m2/s, transference number from ~0.35 to 0.45
2. **Rationale**: High-transport electrolyte eliminates lithium plating during 4C fast charge (anode potential stays positive)

### Why Changes Were Made
- Baseline Chen2020 system showed lithium plating during 4C charge (anode potential -0.44V)
- Three architecture variants (thick/thin/porosity) all failed to eliminate plating
- Electrolyte transport improvement was identified as the only viable path to eliminate plating

### What Could Not Be Achieved
1. **Thermal Constraint (50°C at 45°C ambient)**: Physically incompatible with 4C fast charge. Minimum temperature rise for 4C charge is ~30°C, making 50°C limit unreachable at 45°C ambient.
2. **Energy Density (950 Wh/L)**: Chen2020 system ceiling is ~850 Wh/L. Would require high-capacity materials (SiOx anode) not in current parameter set.
3. **Voltage Plateau (4.1V)**: Chen2020 NMC811 peaks at ~4.04V. Would require higher-voltage cathode (e.g., LNMO 4.7V).

### Recommendations for Future Design
1. Relax thermal constraint to 80°C maximum for 4C charge at 45°C ambient
2. Use OKane2022 parameter set with SiOx anode for higher energy density
3. Consider LNMO high-voltage cathode for 4.1V+ plateau