# Technical Datasheet — GridStore-D3

Number: VBF-T2R1-DSH-01    Case: t2_r1 (grid energy storage)    Date: 2026-08-25

All values mechanically taken from simulation outputs / parameter set; sources per row.

| Field | Value | Source |
| --- | --- | --- |
| Rated capacity (Ah) | 5.0 nominal (parameter set); 5.066 simulated 1C discharge | Chen2020 dump; cell/r6_d3_1c.json:capacity_ah |
| Nominal voltage / voltage window (V) | 2.5 – 4.2 V; discharge plateau proxy 3.722 V at fixed t = 1800 s of 1C | Chen2020 dump; r6_d3_1c.json (calc-energy 'midpoint' scalar is a solver-step-density index artifact — see design_spec §6) |
| Rated energy (Wh) | 18.454 (time integration of V·I at 1C) | cell/r6_d3_energy.json:energy_wh |
| Energy density | 465.62 Wh/kg (contract caliber, electrolyte excluded); 894.87 Wh/L | cell/r6_d3_energy.json:energy_density_wh_kg / _wh_l |
| Maximum continuous discharge rate | 1C (5.066 A) simulated; higher rates not in task contract (5C protocol not run) | cell/r6_d3_1c.json |
| Fast-charge capability | 4C charge @ 45 °C: plating-free (anode potential min +0.0498 V), acceptance 0.838 Ah to 4.2 V, T_max 342.39 K (+24.2 K above ambient) | cell/r6_d3_4c.json:anode_potential_v / capacity_ah / T_max_K |
| Operating temperature range | Verified −20 °C (253.15 K) to +45 °C (318.15 K) per simulation conditions; −20 °C discharge retention 99.571% (protocol and true-soak, cell temp 266.7 K) | cell/r6_d3_lowT_ret.json; cell/r6_d3_lowT_soak.json |
| Cycle life | Aging protocol (1C CC 2.5–4.2 V, SEI ec-reaction-limited, isothermal): SEI thickness 9.087 nm after 100 cycles, 25.317 nm after 500 cycles (contract limits 500/550 nm); capacity trajectory flat. Honest annotation: the reported per-cycle capacity variable is a PyBaMM artifact (freezes at first-discharge value); probe confirms real steps are full 1C swings (5.08 Ah discharge / 4.75 Ah charge per cycle) | cell/r6_d3_aging100.json / r6_d3_aging500.json; bridge/probe_aging.py |
| Safety determination | 4C fast charge plating-free; T_max 342.39 K during 4C charge (no contract red line); abuse scenarios (nail / overcharge / crush) not simulated — N/A (beyond pure simulation boundary) | cell/r6_d3_4c.json |
| Dimensions and mass | 1580 × 65 × 0.2008 mm (W × H × T, layer stack); 39.63 g contract caliber (electrolyte excluded); shell/casing Not provided | Chen2020 dump; cell/r6_d3_energy.json:mass_kg / thickness_m |