# Technical Datasheet — Power-Tool Battery Cell (V8)

Document no.: VBF-T3R1NOFORCE-DSH-01 · Case exp/t3_r1_noforce · 2026-08-25

| Field | Value | Source |
| --- | --- | --- |
| Rated capacity (Ah) | 3.0 (design rating) / 2.6683 simulation-verified at 1C | bridge/params_v8.json / cell/r4_v8_1c_dfn.json |
| Nominal voltage / voltage window (V) | midpoint 3.9215; window 2.5 - 4.2 | cell/r4_v8_energy.json / Chen2020 cut-offs |
| Rated energy (Wh) | 9.833 | cell/r4_v8_energy.json:energy_wh |
| Energy density | 311.0 Wh/kg / 651.3 Wh/L | cell/r4_v8_energy.json (contract mass formula, electrolyte excluded) |
| Maximum continuous discharge rate | 5C (15 A): capacity 2.6261 Ah, retention 0.9842 vs 1C | cell/r4_v8_5c_dfn.json / cell/r4_v8_derived.json |
| Fast-charge capability | 4C (12 A) at 45 C ambient: T_max 323.57 K, anode potential min +0.0119 V -> no plating | cell/r4_v8_4c45_dfn.json |
| Operating temperature range | Simulated: 298.15 K discharge / 318.15 K charge ambient (protocol conditions); broader range not simulated | protocol definitions |
| Cycle life | Not simulated (requires aging model) | honest annotation per protocol |
| Safety determination | No plating on 4C charge; T_max 323.57 K <= 333.15 K (60 C) | cell/r4_v8_5c_dfn.json / cell/r4_v8_4c45_dfn.json |
| Power density (W/kg) | 73121.8 | cell/r4_v8_energy.json |
| Dimensions and mass | electrodes 65 x 1580 mm (unrolled), stack 0.147 mm; mass 31.6 g (contract, electrolyte excluded; 37.6 g incl. electrolyte fill); shell Not provided | Chen2020 + params_v8.json + cell/r4_v8_energy.json |