# Technical Datasheet - VBF-T3R3-DSH-01

Power-tool battery cell (NMC811 / graphite, Chen2020 parameter set; champion V12-HiP-final). All values from simulation tool outputs; per-line sources in the value column.

| Field | Value / source |
| --- | --- |
| Rated capacity (Ah) | 5.0 Ah nominal (parameter set); 4.32 Ah verified at 1C (DFN simulation) - meets >= 2 Ah |
| Nominal voltage / voltage window (V) | 1C midpoint 3.778 V (simulated); window 2.5-4.2 V (parameter set) |
| Rated energy (Wh) | 15.70 Wh (V*I time integral over 1C discharge) |
| Energy density (Wh/kg / Wh/L) | 706.3 Wh/kg (contract caliber, electrolyte excluded); 994.1 Wh/L |
| Maximum continuous discharge rate | 5C verified: capacity retention 98.62% (>= 95% required), T_max 319.57 K (46.4 C) |
| Fast-charge capability | 4C CC charge at 45 C ambient: T_max 329.75 K (56.6 C) <= 333.15 K; anode potential min +41.7 mV -> no lithium plating. Honest note: CC acceptance 0.811 Ah before the 4.2 V ceiling (effective ~4.6C vs 5 Ah nominal). |
| Operating temperature range | Simulated at 25 C discharge / 45 C charge ambient; peak simulated temperature 56.6 C <= 60 C limit (lumped thermal) |
| Cycle life | Not simulated (requires aging protocol; aging-capable parameter set available) |
| Safety determination | 4C fast charge: plated = false (anode min +41.7 mV > 0); peak temperature 56.6 C within 60 C |
| Dimensions and mass | Layer stack 153.8 um x 65 mm x 1.580 m wound strip (parameter-set geometry); stack mass 22.23 g (calc-energy contract formula, electrolyte excluded; 8.93 g electrolyte fill; enclosure/tabs not modeled - shell dimensions Not provided) |

Released under the Virtual Battery Factory delivery package; see calc.xlsx for the derivation chain and design_spec.md for design rationale.